NGHIÊN CỨU ĐIỀU CHẾ HỆ PHÂN TÁN RẮN CỦA ALTRETAMIN

BẰNG PHƯƠNG PHÁP ĐUN CHẢY

Dương Quốc Toản*, Trịnh Nam Trung**,

Nguyễn Duy Bắc**, Vũ Bình Dương**

SUMMARY

STUDY ON PREPARING OF

ALTRETAMINE SOLID DISPERSION SYSTEM BY MELTING METHOD

We have successfully prepared solid dispersion system containing Altretamine by melting method using PEG 6000 as carrier. The selection of carrier and solubility enhancer of drug in solid dispersion system showed that: PEG 6000 at the ratio (to drug) of 1 :1 as a carrier, supplemented with 0.5% tween 80 increased the solubility of Altretamine 3.28 folds compared with original material. Drug releasing rate was significantly improved, after 5 minutes reached 45.51% and after 60 minutes reached 62.05% compared with 3.28% and 17.09% of raw Altretamine. Thus we can use solid dispersion system of Altretamine prepared by melting method using PEG as carrier in preparation of drug solid form containing Altretamine to enhance the effectiveness of Altretamine.

Keywords: Altretamine, solid dispersion system.